## Slide 1: AI 4 Materials Design
September 3, 2025
Caleb Morgan; Solomon Boakye-Yiadom
Mechanical Engineering
York University

## Slide 2: Course Objective
To provide a comprehensive introduction into the application of machine learning to the design and discovery of new materials
  Conceptual & mathematical foundations
  Examples & case studies
  Hand-on practice

## Slide 3: Learning Outcomes
At the conclusion of this course, the student should be able to:
  Recognize, define and describe key concept in machine learning approaches of relevance to materials science.
  Analyze and understand given data pertaining to a materials science problem.
  Apply machine learning algorithms for understanding structure-property relations in materials science, and materials design and discovery
  Integrate above knowledge to solve practical materials science problems using machine learning and demonstrate it through projects and research

## Slide 4: Pre-requisites
Knowledge of basic statistics (e.g., statistical distributions, Bayes’ theorem, regression etc.)
Knowledge of basic linear algebra (e.g., matrix multiplications, eigen value decompositions, inverses)
Some programming experience, ideally Python
Knowledge of materials structure and property concept

## Slide 5: Essential Work of Materials Science
Materials Science develops the fundamental understanding of relationships and structure of materials
Materials Engineering uses this understanding to engineer (design) materials for real-life application

## Slide 6: PSPP Relationship of Materials
Agrawal, A., & Choudhary, A. (2019). Deep materials informatics: Applications of deep learning in materials science. MRS Communications, 9(3), 779–792. https://doi.org/10.1557/MRC.2019.73/FIGURES/6

## Slide 7
Stone Age
Bronze Age
Iron Age
Middle Age
Info. Age
2.5M – 3000 BCE
Obsidian, flint, + animal hide, bone, wood, found hydrocarbons
3000 – 1200 BCE
Bronze, + clay ceramics, papyrus, gold, silk, rubber
1200 BCE – 300 CE
Iron, + steel, glass, processed minerals
300 – 1300 CE
Porcelain ceramic (Far East), + ceramic glazes, lacquer, metal/ceramic composites
Industrial Era
1300 – 1950 CE
Steel, + aluminum and other metals, alloys of same, synthetic polymers, extracted hydrocarbons
1950 CE - ???
Silicon, + modern composites, polymers, nanostructured materials “metamaterials”
Materials Development by Era
Different eras in human history are named after the materials incorporated in the predominant technologies

## Slide 8: Materials Science Paradigms through Ages
Agrawal, A., & Choudhary, A. (2019). Deep materials informatics: Applications of deep learning in materials science. MRS Communications, 9(3), 779–792. https://doi.org/10.1557/MRC.2019.73/FIGURES/6

## Slide 9: Materials Science from “First-Principles”
Material Properties
Phase stability
Diffusion barriers
Surface energies and Wulff shape
Material properties
Electronic structure
Charge densities
Schrodinger Equation
Generally applicable to any chemistry
Inherently scalable
Density functional theory (DFT) approximation

## Slide 10: Materials Science Paradigms through Ages
Lejaeghere, K., Bihlmayer, G., Björkman, T., Blaha, P., Blügel, S., Blum, V., Caliste, D., Castelli, I. E., Clark, S. J., Dal Corso, A., de Gironcoli, S., Deutsch, T., Dewhurst, J. K., di Marco, I., Draxl, C., Dułak, M., Eriksson, O., Flores-Livas, J. A., Garrity, K. F., … Cottenier, S. (2016). Reproducibility in density functional theory calculations of solids. Science, 351(6280). https://doi.org/10.1126/SCIENCE.AAD3000/SUPPL_FILE/AAD3000-LEJAEGHERE-SM.PDF

## Slide 11: Where does Data Science lie?

## Slide 12: Data Explosion

## Slide 13: Expanding Database of “computed” properties
Chen, C., Zuo, Y., Ye, W., Li, X., Deng, Z., Ping Ong, S., Chen, C., Zuo, Y., Ye, W., Li, X., Deng, Z., & Ong, S. P. (2020). A Critical Review of Machine Learning of Energy Materials. Advanced Energy Materials, 10(8), 1903242. https://doi.org/10.1002/AENM.201903242
Number of crystal structures with various properties computed in Materials Project since inception

## Slide 14: ML & Big Data
Zhou, T., Song, Z., & Sundmacher, K. (2019). Big Data Creates New Opportunities for Materials Research: A Review on Methods and Applications of Machine Learning for Materials Design. Engineering, 5(6), 1017–1026. https://doi.org/10.1016/J.ENG.2019.02.011
Number of published works on “machine learning” and “machine learning” + “material” (from January 1999 to September 2018)
Number of published works on “big data” and “data-driven” methods (from January 1999 to September 2018)

## Slide 15: Materials Ontology
Himanen, L., Geurts, A., Foster, A. S., & Rinke, P. (2019). Data-Driven Materials Science: Status, Challenges, and Perspectives. Advanced Science, 6(21), 1900808. https://doi.org/10.1002/ADVS.201900808
Example of an ontological hierarchy for the structural characterization of materials: a materials tree of life.

## Slide 16: Basic Machinery of Machine Learning in Materials Design

## Slide 17: Key Steps in Building a ML Model
Himanen, L., Geurts, A., Foster, A. S., & Rinke, P. (2019). Data-Driven Materials Science: Status, Challenges, and Perspectives. Advanced Science, 6(21), 1900808. https://doi.org/10.1002/ADVS.201900808
Key steps in building a machine learning model. The white arrows indicate the flow of data; green arrows indicate actions that can be identified and performed after analysis to improve the performance of the model

## Slide 18: Workflow of ML for Materials Design
Chen, C., Zuo, Y., Ye, W., Li, X., Deng, Z., Ping Ong, S., Chen, C., Zuo, Y., Ye, W., Li, X., Deng, Z., & Ong, S. P. (2020). A Critical Review of Machine Learning of Energy Materials. Advanced Energy Materials, 10(8), 1903242. https://doi.org/10.1002/AENM.201903242

## Slide 19: Illustrative examples of application of machine learning in materials science

## Slide 20: Application area: physical metallurgy (HEA) Property: hardness

## Slide 21
Application area: Refractory CCA
Property: strength at high temperatures, hardness
Zhang, C., Gu, X., Bhandari, U., Lei, J., Guo, S., Kourouma, M., Karoui, A., Yang, S., Pradeep, K. G., & Singh, P. (2022). Machine learning prediction of the mechanical properties of refractory multicomponent alloys based on a dataset of phase and first principles simulation. Frontiers in Metals and Alloys, 1, 1036656. https://doi.org/10.3389/FTMAL.2022.1036656
CALPHAD was used to check phase stability and generate phase diagrams for potential compositions
Employs DFT to calculate material properties and select relevant features correlated with alloy behavior

## Slide 22
Application area: lightweight refractory HEAs
Property: hardness, corrosion resistance, light weight
Gao, T., Gao, J., Yang, S., & Zhang, L. (2024). Data-driven design of novel lightweight refractory high-entropy alloys with superb hardness and corrosion resistance. Npj Computational Materials 2024 10:1, 10(1), 1–13. https://doi.org/10.1038/s41524-024-01457-6

## Slide 23: Module Summary
AI/ML in Materials Science: A relatively new field, emerging within the past 5 years
Rapid Advancement: While machine learning has been a longstanding discipline, its integration into materials science has seen explosive growth over the last decade.
Industry Interest: Despite significant interest from the materials industry, large-scale applications are still in the early stages.
Initial Successes: Early research has yielded promising results in more approachable and foundational areas.
Challenges Ahead: More complex and challenging problems are now being addressed, pushing the boundaries of the field.
Data & Tools Expansion: The development of comprehensive databases and analytical tools continues to fuel growth and innovation.